## Slide 1: Electroless plating
Dr. Rani Pavithran
Assistant Professor & Head
Department of Chemistry
College of Engineering Trivandrum

## Slide 2: Electroless plating
It is a controlled autocatalytic deposition of a continuous layer of a noble metal from its salt solution on a catalytic surface of the base metal by using a suitable reducing agent without using electrical energy.
This method allows the easy preparation of thin films using simple equipment.
Electroless deposition is an autocatalytic process where the substrate develops a potential in a plating bath containing metallic ions, reducing agent, complexing agent, stabilizer and other components.

## Slide 3
This is a non-galvanic plating method that involves several simultaneous reactions in an aqueous solution, which occur without the use of external electrical power.
The reaction is accomplished when hydrogen is released by a reducing agent, normally sodium hypophosphite (the hydrogen leaves as a hydride ion), and oxidized, thus producing a negative charge on the surface of the metal or part.
The key requirement of an electroless deposition bath of this type is to arrange the chemistry such that the kinetics of homogeneous electron transfer from the reducing agent to the metal ion is slow.
This is essential because otherwise the metal ion would simply be reduced in the bulk solution.
Principle

## Slide 4: Stability of plating
The stability of electroless plating fully depends on the substrate material, the pretreatment process, the type of solution used, the pH and temperature during plating.
A catalyst that accelerates the rate of metal ion reduction is thus applied to the surface to be coated.
In this way, metal ions are reduced only at the surface and the surface becomes coated with the desired metal.

## Slide 5: Process of Electroless plating
Steps involved in the process of electroless plating:
step1. Preparation of the surface to be plated: In this step the surface is activated by following ways
(a) Etching- Removal of impurities by acid treatment.
(b) Electroplating - A thin layer of the metal to be plated or any other suitable metal is coated on the surface of the object.
(c) Chemical Treatment- The plastic objects and printed circuit boards are treated with SnCl2 and PdCl2. This treatment yields a thin layer of Pd on the treated surface.

## Slide 6: Process of Electroless plating
Step 2. Preparation of plating bath: The plating bath should include the following
(a) Soluble salt of the metal (like chloride or sulphate)
(b) Complexing agents like EDTA, tartarate, citrate etc. to prevent excess deposition.
(c) Reducing agents like sodium thiosulphite, formaldehyde etc
(d) Exaltants or accelerators like succinates, glycinates, fluorides etc to enhance the plating rate.
(e) Stabilizers like calcium ions, lead ions, thio urea etc. to prevent decomposition of the bath and to impart stability to the solution.
(f) Buffer solution like Rochelle salt, Boric acid to maintain pH.

## Slide 7: Process of Electroless plating
Step 3
Procedure:
The article to be plated is immersed in the bath containing the metal salt and reducing agent.
The plating is carried out in a series of tanks.
The rate of deposition is controlled by the amount of reducing agent and the type of chelating agent.

## Slide 8: Advantages
1. Surface to be coated does not need to be conductive, thus electroless plating can be made on both metals and plastics.
2. Electrical power and other accessories are not required
3. Gives uniform coating even on the objects with irregular shapes, holes recesses etc.
4. Coating provides better wear resistance.
5. The coating is less porous and provides better corrosion resistance.
6. Provides flexibility in plating volume and thickness

## Slide 9: Electroless Copper plating
Electroless copper plating is used to deposit a layer of copper on a substrate without the use of electrical energy.
It is commonly used for making printed circuit boards.
1. The object to be plated is degreased using organic solvent
2. This is followed by acid treatment.
3. This object is then immersed in plating bath containing cupric salt, reducing agents, buffer and complexing agent.

## Slide 10: Electroless Copper plating
At cathode
At anode
Overall reaction (1) + (2)
Electroless copper solutions, utilizing formaldehyde as reducing agent, employ high pH, above 12 (typical NaOH concentration is > 0.1N; pH above 13)

## Slide 11: Electroless Copper plating
Uses
1. This type of coating is mainly used in double or multi-layerd printed circuit boards in which plating through holes is required.
2. This is used as base coating for subsequent electroplating.

## Slide 12: Electroless Nickel Plating
Metals like Al, Fe, Cu and alloys like brass are plated with nickel.
Non-metallic materials like glass, plastic and quartz are pretreated with SnCl2 in acid medium followed by treatment with PdCl2 solution.
The pretreated object is immersed in the plating bath containing nickel salt and reducing agent like sodium hypophosphite for a certain time so that following reactions will occur and nickel gets coated over the object.

## Slide 13: Electroless Nickel Plating
At cathode
At anode
Overall reaction (1) + (2)
As H+ ions are released in the reaction, pH of the solution decreases.
To maintain constant pH, buffer solutions are generally used.
This gives a uniform fine grained plating.

## Slide 14: Electroless Nickel Plating
Uses
In Aerospace Components: For wear resistance, corrosion protection, chemical resistivity and lubricity on valves, pistons, engine shafts, engine mounts, compressor blades etc.
2. In packaging and handling machinery: Due to its wear resistance, cleanliness and attractive finish.
3. In chemical manufacturing: Due to chemical resistance used in chemical manufacturing and storage equipments.
4. In Automotive Components: For wear protection and corrosion resistance on pistons, cylinders, gears, differential opinon ball shafts, fuel injectors, ball studs, heat sinks and others.